## Slide 1: Modelisation of laser pulse heating of TiN/GST/Si layers
Simon Schmit, July 2025

## Slide 2: Heat input profile (beam modelling) and parameters
Updated 2D Gaussian heat input :
Parameters :

## Slide 3: Geometry and mesh of the layers
GST225
Si
TiN

## Slide 4: Temperature gradient at the end of the pulse
TiN
Ge2Sb2Te5
Si
Substrate (1500nm)
100 nm
20 nm

## Slide 5: Temperature gradient at the end of the pulse
Substrate (1500nm)
100 nm
20 nm

## Slide 6: Temperature vs time at the middle of the laser beam on TiN layer surface (x=0, y=0)

## Slide 7: Maximum temperature depending on the laser power
Chart: Maximum temperature vs laser power
| 300 | 350 | 400 | 500 | 750 | 1200 | 200
 | 1310.4 | 1480 | 1649.5 | 1988.6 | 2836.4 | 4362.3 | 971.35
Power (W) | Temperature max (K)
200 | 971.35
300 | 1310.4
350 | 1480
400 | 1649.5
500 | 1988.6
750 | 2836.4
1200 | 4362.3