## Slide 1: Modelisation of laser pulse heating of GST225 and GGSTN layers using COMSOL
Simon Schmit, July 2025

## Slide 2: Plan of the presentation
Configurations 1 and 2
Both configuration
Parameters and properties :
Temperature vs time
Temperature vs depth
Impact of the GST layers thickness
Plateau temperature vs laser power
Single GST layer
Temperature vs time
Temperature vs depth
Characteristic time

## Slide 3: Parameters and properties: materials and geometry
Properties | a-GST | c-GST | a-GGSTN | c-GGSTN
A : Absorption coefficient for 1070 nm (1/m) | 8.76E+06 | 3.78E+07 | 4.28E+06 | 1.33E+07
k : Thermal conductivity W/(m*K) | 0.2 | 0.45 | 0.28 | 1.8
GST layers properties
GST (5 nm)
GGSTN (45 nm)
TiN (20 nm)
Si (substrate)
GST (5 nm)
GGSTN (45 nm)
TiN (20 nm)
Si (substrate)
Configuration 1
Configuration 2
1000 um length
1000 um length

## Slide 4: Parameters and properties: simulation parameters
Gaussian heat input
Thermal profile
Laser parameters
Beam x-radius | 170 um
Beam y-radius | 150 um
Power | 300 W
Pulse duration | 1 us
Wavelength | 1700 nm
Fluence | 0.3745 J/cm²
Mesh

## Slide 5: Configuration 1: temperature vs time (x=0,y=0,z=0)
100 nm
20 nm
Chart: Time (s)
| 0 | 5.7603000000000003E-10 | 1.1481E-9 | 2.2921E-9 | 3.4362000000000002E-9 | 5.7243000000000002E-9 | 8.0123999999999993E-9 | 1.03E-8 | 1.4877E-8 | 1.9452999999999999E-8 | 2.4029E-8 | 3.3181999999999999E-8 | 4.2334E-8 | 6.0639000000000005E-8 | 7.7112999999999997E-8 | 9.3588000000000004E-8 | 1.1005999999999999E-7 | 1.4301000000000001E-7 | 2.0891000000000001E-7 | 2.7481000000000001E-7 | 3.9999999999999998E-7 | 4.9999999999999998E-7 | 5.9999999999999997E-7 | 6.9999999999999997E-7 | 7.9999999999999996E-7 | 8.9999999999999996E-7 | 9.3766999999999995E-7 | 9.5650999999999993E-7 | 9.9418000000000003E-7 | 9.9889000000000002E-7 | 1.0033E-6 | 1.0067E-6 | 1.0102000000000001E-6 | 1.0135999999999999E-6 | 1.0205E-6 | 1.0273000000000001E-6 | 1.0410000000000001E-6 | 1.0530999999999999E-6 | 1.0652E-6 | 1.0772E-6 | 1.0893000000000001E-6 | 1.1134E-6 | 1.1375999999999999E-6 | 1.1858999999999999E-6 | 1.2824E-6 | 1.3790000000000001E-6 | 1.5E-6 | 1.5999999999999999E-6 | 1.7E-6 | 1.7999999999999999E-6 | 1.9E-6 | 1.9999999999999999E-6
Amorphous | 293.25 | 304.94 | 317.3 | 343.48 | 370.75 | 420.53 | 461.92 | 497.63 | 552.3 | 594.36 | 626.96 | 676.57 | 707.49 | 741.9 | 754.18 | 759.66 | 762.59 | 766.08 | 766.91 | 767.12 | 767.24 | 767.24 | 767.23 | 767.22 | 767.22 | 767.22 | 767.22 | 767.22 | 767.22 | 734.61 | 642.31 | 582.84 | 535.24 | 496.68 | 435.28 | 393.69 | 343.55 | 323.06 | 312.54 | 306.45 | 302.49 | 297.31 | 294.79 | 293.15 | 293.15 | 293.15 | 293.16 | 293.16 | 293.15 | 293.15 | 293.15 | 293.15
Crystalline | 293.25 | 302.36 | 310.93 | 327.43 | 351.71 | 367.03 | 377.3 | 389.35 | 397.4 | 407.6 | 414.85 | 423.77 | 429.38 | 434.62 | 437.04 | 438.52 | 438.95 | 439.08 | 439.12 | 439.12 | 439.12 | 439.12 | 439.12 | 379.61 | 308.93 | 295.49 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15

## Slide 6: Configuration 1/ amorphous phase: temperature vs depth (10-8 m) (x=0, y=0)
100 nm
20 nm
Si
GST
GGSTN
TiN

## Slide 7: Configuration 1/ crystalline phase: temperature vs depth (10-8 m) (x=0, y=0)
100 nm
20 nm
Si
GST
GGSTN
TiN

## Slide 8: Configuration 2: temperature vs time (x=0,y=0,z=0)
100 nm
20 nm
Chart: Time (s)
| 0 | 5.6641557736989503E-10 | 1.1288311547397901E-9 | 2.2536623094795801E-9 | 4.5033246189591599E-9 | 6.7529869284387401E-9 | 9.0026492379183202E-9 | 1.12523115473979E-8 | 1.5751636166357E-8 | 2.0250960785316199E-8 | 2.9249610023234499E-8 | 3.8248259261152797E-8 | 5.6245557736989498E-8 | 7.4242856212826099E-8 | 1.10237453164499E-7 | 1.46232050116172E-7 | 2.1822124401951899E-7 | 2.90210437922865E-7 | 3.9999999999999998E-7 | 4.9999999999999998E-7 | 5.9999999999999997E-7 | 6.9999999999999997E-7 | 7.9999999999999996E-7 | 8.9999999999999996E-7 | 9.9999999999999995E-7 | 1.07991804599021E-6 | 1.1313142233143499E-6 | 1.18271040063849E-6 | 1.2341065779626301E-6 | 1.33689893261091E-6 | 1.5E-6 | 1.5999999999999999E-6 | 1.6999999999999901E-6 | 1.7999999999999999E-6 | 1.9E-6 | 1.9999999999999999E-6
Crystalline | 293.2464 | 302.9611 | 312.0835 | 329.4148 | 354.1998 | 369.2871 | 379.1125 | 385.9984 | 394.7912 | 401.1491 | 409.8709 | 416.3442 | 424.5229 | 429.7461 | 434.7177 | 437.0524 | 438.5061 | 438.9373 | 439.0816 | 439.1193 | 439.122 | 439.1194 | 439.118 | 439.1177 | 379.1917 | 308.7715 | 295.7648 | 293.1502 | 293.15 | 293.15 | 293.15 | 293.1513 | 293.1527 | 293.151 | 293.1501 | 293.15
Amorphous | 293.26 | 306.02 | 318.86 | 345.62 | 399.92 | 445.77 | 485.13 | 551.97 | 602.89 | 673.03 | 713.58 | 737.2 | 751.58 | 760.9 | 773.06 | 779.41 | 785.92 | 786.56 | 786.97 | 787.14 | 787.18 | 787.18 | 787.18 | 787.18 | 787.18 | 787.18 | 787.18 | 787.18 | 787.18 | 786.93 | 757.88 | 683.94 | 625.57 | 543.57 | 493.84 | 455.39 | 425.42 | 379.56 | 350.65 | 318.12 | 307.29 | 301.96 | 298.88 | 296.89 | 294.42 | 293.4 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15

## Slide 9: Configuration 2/ amorphous phase: temperature vs depth (10-8 m) (x=0, y=0)
100 nm
20 nm
Si
GST
GGSTN
TiN

## Slide 10: Configuration 2/ crystalline phase: temperature vs depth (10-8 m) (x=0, y=0)
100 nm
20 nm
Si
GST
GGSTN
TiN

## Slide 11: Plateau temperature vs laser power
100 nm
20 nm
Chart: Laser Power (W)
| 100 | 200 | 300 | 400 | 500 | 600
Amorphous | 457.93 | 609.2 | 767.23 | 925.25 | 1083.3 | 1241.3
Crystalline | 341.81 | 390.46 | 439.12 | 487.77 | 536.43 | 585.09
Laser Power (W) | Amorphous temperature (K) | Crystalline temperature (K)
100 | 457.93 | 341.81
200 | 609.2 | 390.46
300 | 767.23 | 439.12
400 | 925.25 | 487.77
500 | 1083.3 | 536.43
600 | 1241.3 | 585.09
Pulse duration : 1 us

## Slide 12: Only GGSTN layer (300W, 1us)
Temperature vs time
Chart: Time (s)
| 0 | 5.0072E-10 | 9.9744000000000002E-10 | 1.9908999999999998E-9 | 2.9843000000000001E-9 | 4.9712000000000004E-9 | 6.9580999999999998E-9 | 8.945E-9 | 1.2919E-8 | 2.0866E-8 | 2.8813999999999999E-8 | 4.4709E-8 | 6.0604000000000005E-8 | 9.2394E-8 | 1.2417999999999999E-7 | 1.8776000000000001E-7 | 2.5134000000000003E-7 | 3.7851000000000002E-7 | 4.9999999999999998E-7 | 5.9999999999999997E-7 | 6.9999999999999997E-7 | 7.9999999999999996E-7 | 8.9999999999999996E-7 | 9.5456999999999995E-7 | 9.9083999999999994E-7 | 9.9705000000000005E-7 | 9.9837999999999992E-7 | 9.9995999999999991E-7 | 1.0015000000000001E-6 | 1.0031E-6 | 1.0047000000000001E-6 | 1.0078999999999999E-6 | 1.0109999999999999E-6 | 1.0173E-6 | 1.0236E-6 | 1.0362999999999999E-6 | 1.0489E-6 | 1.0742E-6 | 1.0994E-6 | 1.1499E-6 | 1.2004E-6 | 1.3014999999999999E-6 | 1.5E-6 | 1.5999999999999999E-6 | 1.7E-6 | 1.7999999999999999E-6 | 1.9E-6 | 1.9999999999999999E-6
Crystalline | 293.25 | 306.28 | 316.35 | 332.38 | 343.54 | 357.98 | 365.91 | 370.86 | 378.15 | 386.5 | 393.24 | 402.35 | 408.45 | 414.63 | 417.73 | 419.83 | 420.51 | 420.79 | 420.85 | 420.85 | 420.84 | 420.84 | 420.84 | 420.84 | 420.84 | 420.84 | 420.84 | 408.64 | 384.58 | 369.6 | 359.71 | 348.4 | 341.04 | 331.77 | 325.01 | 315.89 | 309.47 | 302.28 | 298.26 | 295.1 | 293.9 | 293.31 | 293.16 | 293.15 | 293.15 | 293.15 | 293.15 | 293.15
Amorphous | 293.25 | 309.93 | 325.01 | 352.85 | 397.62 | 436.37 | 470.16 | 528.19 | 573.25 | 636.62 | 674.59 | 697.57 | 712.04 | 721.69 | 734.5 | 741.5 | 749.03 | 750.22 | 750.85 | 751.31 | 751.51 | 751.57 | 751.56 | 751.56 | 751.56 | 751.56 | 751.56 | 751.56 | 751.56 | 751.56 | 751.56 | 699.22 | 650.78 | 578.25 | 527.07 | 486.48 | 454.07 | 403.26 | 369.81 | 330.49 | 315.49 | 307.77 | 303.18 | 300.11 | 296.11 | 294.21 | 293.15 | 293.15 | 293.15 | 293.16 | 293.16 | 293.15 | 293.15 | 293.15 | 293.15
GGSTN (50 nm)
TiN (20 nm)
Si (substrate)
1000 um length
Configuration

## Slide 13: Only GGSTN layer (300W, 1us): temperature vs depth (10-8 m)
Crystalline
Amorphous
TiN
GGSTN
Si
TiN
GGSTN
Si

## Slide 14: Only GST layer (300W): characteristic time
GST (100 nm)
TiN (20 nm)
Si (substrate)
1000 um length
Configuration
Chart: Characteristic time vs the pulse duration
| 10 | 100 | 250 | 400 | 500 | 750 | 1000
Characteristic time | 4.9e-09 | 2.3e-08 | 3.56e-08 | 3.59e-08 | 3.59e-08 | 3.59e-08 | 3.59e-08
Pulse duration | Characteristic time
10 | 4.90E-09
100 | 0.000000023
250 | 3.56E-08
400 | 3.59E-08
500 | 3.59E-08
750 | 3.59E-08
1000 | 3.59E-08