## Slide 1: Impact of GGSTN properties and layers alternation
Simon Schmit, July 2025

## Slide 2
IMPACT OF THE ABSORPTION COEFFICIENT
GGSTN Absorption (1/m) | Maximum temperature (K) | Slope of temp vs depth (K/nm)
4.28E+05 | 1082.4 | -12.33
4.28E+06 | 1199.2 | -13.96
4.28E+07 | 1395.6 | -16.89
Chart: Maximum temperature vs GGSTN absorption
| 428000 | 4280000 | 42800000
Maximum temperature vs GGSTN absorption | 1082.4 | 1199.2 | 1395.6
Chart: Slope of GGSTN in depth vs absorption
| 428000 | 4280000 | 42800000
Slope of GGSTN in depth vs absorption | -12.33 | -13.96 | -16.89
Configuration :
GGSTN first (45 nm)
1300W
1us pulse duration
350 um beam radius

## Slide 3
Impact of the Thermal Conductivity
Chart: 
| 0.2 | 0.28000000000000003 | 0.4 | 0.1
Maximum temperature vs GGSTN conductivity | 976.61 | 828.44 | 717.53 | 1494.4
Chart: Slope of GGSTN temperature in depth vs thermal conductivity
| 0.2 | 0.28000000000000003 | 0.4 | 0.1
Slope of GGSTN temperature gradient vs thermal conductivity | -11.55 | -8.25 | -5.78 | -23.1
Maximum temperature | GGSTN Thermal conductivity | Slope of GGSTN (temp vs depth) (K/nm)
976.61 | 0.2 | -11.55
828.44 | 0.28 | -8.25
717.53 | 0.4 | -5.78
1494.4 | 0.1 | -23.1
Configuration :
GGSTN first (45 nm)
1300W
1us pulse duration
350 um beam radius

## Slide 4
Layer alternation : temperature vs depth at t=1us
GST (5 nm)
GGSTN (5 nm)
TiN (20 nm)
Si (substrate)
50 nm
1700 um

## Slide 5
Layer alternation : temperature in the middle of the TiN surface
GST (5 nm)
GGSTN (5 nm)
TiN (20 nm)
Si (substrate)
50 nm
1700 um

## Slide 6
Layer alternation : heat input (W/m^3) vs depth at t=1us
GST (5 nm)
GGSTN (5 nm)
TiN (20 nm)
Si (substrate)
50 nm
1700 um

## Slide 7
2500W Laser : classic configuration

## Slide 8
2500W Laser : classic configuration